Increasing the autonomy of electrical MAV:

Design of a new electrochemical generator featuring high specific power and energy

D. GOFFE, C. KIRRMANN (BERTIN Technologies)

D. MARSACQ et E. DAMERY (CEA/LITEN)

Abstract

The high energy needed for powering electrical MAV can be obtained by using Aluminum-air Fuel cells, which have a high potential energy to mass ratio.

Such batteries can reach more than 250 Wh/kg, while lithium-polymer batteries are currently limited to around 160 Wh/kg.

A 100 W prototype is being developed to power small UAV up to 1000 g.

The technical concepts of the Al/air fuel cell are described and the performances obtained with the first prototypes are discussed.